## Slide 1: Quo vadis caementum – nothing goes without rheology
Dr.-Ing. D. Hornung, Dyckerhoff AG Wiesbaden, Portfoliomanagement & Anwendungsberatung
Kolloquium Rheologische Messungen an mineralischen Baustoffen, Regensburg 29.02.2012

## Slide 2: Content
Sustainability – Modern trends or duty of enterprise strategy?
Cement production and CO2 emission – CEM II and CEM III become standard
M-cements – optimised for performance, durable and uniform
Rheology of cement paste vs. cement standard parameters
Rheology of cement paste – Experience from 5 years RheoZ
Summary

## Slide 3: CO2 Ranking industry
Cement industry
CO2-Emission

## Slide 4: Cement Technology Roadmap 2009
No alternative clinker concepts !

## Slide 5: Content
Sustainability – Modern trends or duty of enterprise strategy?
Cement production and CO2 emission – CEM II and CEM III become standard
M-cements – optimised for performance, durability and uniformity
Rheology of cement paste vs. cement standard parameters
Rheology of cement paste – Experience from 5 years RheoZ
Summary

## Slide 6
Raw material quarrying
Raw material preparation
Raw material for cement production
CaCO3

## Slide 7
Raw material preparation
Clinker sintering
Emission von 0,85 t CO2/ t Klinker
Brennstoffbed. CO2
0,32 t CO2 pro t Klinker
Prozessbed. / „Entsäuerungs“ - CO2:
CaCO3  CaO + CO2
0,525 t CO2 pro t Klinker
Preparation and sintering
Klinker
1450°C

## Slide 8
Clinker storage
BFS S
Pit coal FA V
Limestone LL
Gypsum
Clinker
CEM II CEM III
CEM IV CEM V
Cement mill
Cement grinding
Trass P
CEM I
„CO2-free“

## Slide 9: CEM II = Standard cements in Germany
CEM II ~ 50%

## Slide 10: Clinker rate – Cements Germany vs. Dyckerhoff
80,6%
75,3%
73,8%
73,9%
71,6%
70,2%
2010
Clinker rate Dyckerhoff
CEM I 66 %
CEM II 19 %
CEM III 15 %
CEM I 33 %
CEM II 42 %
CEM III 25 %
CEM II/B-M
CEM II/B-M
Dyckerhoff
Dyckerhoff

## Slide 11: CEM II = Composite cements
CEM II / CEM III = CEM I + other materials with hydraulic properties
S Blast-furnace slag (finely ground, granulated blast-furnace slag)
V Pit coal fly ash (finely ground/not ground/separated)
LL Limestone (finely ground, increased requirements)
P Trass (finely ground)
Long-time experience with S, V, LL, P in cement/concrete
Expanded normative requirements for cement/concrete
Increased R & D for composites in cement/concrete
Good durability properties

## Slide 12: Reaction of C3S + finely ground limestone
0
6
12
18
24
30
36
Time of hydration [h]
2
3
4
5
6
7
8
9
10
11
12
Rate of heat development [J/gh]
35% KSM
15% KSM
0,40% FM/35% KSM
0,40% FM/15% KSM
0,40% FM
without FM/KSM
Influence of limestone on hydration

## Slide 13: Reaction of C3S + finely ground limestone
Dense C-S-H phase formation
at C3S and limestone surface
Limestone base
Increased C-S-H phase development
ESEM image without and with ground limestone

## Slide 14: Content
Sustainability – Modern trends or duty of enterprise strategy?
Cement production and CO2 emission – CEM II and CEM III become standard
M-cements – optimised for performance, durability and uniformity
Rheology of cement paste vs. cement standard parameters
Rheology of cement paste – Experience from 5 years RheoZ
Summary

## Slide 15: CEM II in cement standard EN 197
Zement | PZ – Klinker Minimum | Hüttensand S Maximum | KalksteinLL Maximum | SFA V Maximum | Trass P Maximum
CEM I | 95 | - | - | - | -
CEM II/A-S | 80 | 20 | - | - | -
CEM II/B-S | 65 | 35 | - | - | -
CEM II/A-LL | 80 | - | 20 | - | -
CEM II/B-LL | 65 | - | 35 | - | -
CEM II/A-V | 80 | - | - | 20 | -
CEM II/B-V | 65 | - | - | 35 | -
CEM II/A-M (S-LL) | 80 | 20 (S + LL) |  | - | -
CEM II/B-M (S-LL) | 65 | 35 (S + LL) |  | - | -
CEM II/A-M (V-LL) | 80 | - | 20 (V + LL) |  | -
CEM II/B-M (V-LL) | 65 | - | 35 (V + LL) |  | -
CEM II/B-P | 65 | - | - | - | 35
CEM III/A, CEM III/B, CEM III/C, CEM IV, CEM V |  |  |  |  | 

## Slide 16
Clinker storage
BFS S
Pit coal FA V
Limestone LL
Gypsum
Clinker
CEM II CEM III
CEM IV CEM V
Cement mill
Cement grinding common milling
Trass P
CEM I
„CO2 free“

## Slide 17
Clinker storage
Ground BFS S
Pit coal FA V
Ground limestone LL
Gypsum
Clinker
CEM II CEM III
CEM IV CEM V
Cement mill
Cement grinding separate milling/mixing
Ground trass P
CEM I
Separate grinding

## Slide 18
Cement grinding
common milling vs. separate milling/mixing
Custom-tailored cements
Advances separate milling/mixíng
Finenesses of components can be adjusted individually
Optimisation of grain size distribution of mixed cements
Optimisation of packing density/water demand/workability
Optimisation of hardening reactions
Improvement of durability
Dyckerhoff CEM II/B-M(S-LL) 32,5 R / 42,5 R / 52,5 R (MZ-S)
Dyckerhoff CEM II/B-M(V-LL) 32,5 R (MZ-V)

## Slide 19
Characteristic LL components
-Acceleration early strength development, heat development
-decreased late strength development
-Inert on durability properties (< 30% ?)
+
Characteristic S, V components
-Decelerated setting/hardening and heat development
-increased late strength development
-Improved durability properties (Pore microstructure and intrusion resistance)
Optimised combination of LL and S/V

## Slide 20
Characteristic LL components
-Acceleration early strength development, heat development
-decreased late strength development
-Inert on durability properties (< 30% ?)
+
Characteristic S, V components
-Decelerated setting/hardening and heat development
-increased late strength development
-Improved durability properties (Pore microstructure and intrusion resistance)
Optimised combination of LL and S/V

## Slide 21
Characteristic LL components
-Acceleration early strength development, heat development
-decreased late strength development
-Inert on durability properties (< 30% ?)
+
Characteristic S, V components
-Decelerated setting/hardening and heat development
-increased late strength development
-Improved durability properties (Pore microstructure and intrusion resistance)
Optimised combination of LL and S/V

## Slide 22: CEM X – Continuation of CEM II/B-M EN 197-1 Expansion / Bauaufsichtliche Zulassung
Cement | PZ – Clinker Minimum | BFS S Maximum |  | Limestone LL Maximum |  | PFA V Maximum | Trass P Maximum
CEM I | 95 | - |  | - |  | - | -
CEM II/A-S | 80 | 20 |  | - |  | - | -
CEM II/B-S | 65 | 35 |  | - |  | - | -
CEM II/A-LL | 80 | - |  | 20 |  | - | -
CEM II/B-LL | 65 | - |  | 35 |  | - | -
CEM II/A-V | 80 | - |  | - |  | 20 | -
CEM II/B-V | 65 | - |  | - |  | 35 | -
CEM II/A-M (S-LL) | 80 | 20 S + LL |  |  |  | - | -
CEM II/B-M (S-LL) | 65 (40-50) | 35 (60-50) S + LL |  |  |  | - | -
CEM II/A-M (V-LL) | 80 | - | 20 V + LL |  |  |  | -
CEM II/B-M (V-LL) | 65 (40-50) | - | 35 (60-50) V + LL |  |  |  | -
CEM II/B-P | 65 | - | - |  | - |  | 35
CEM III/A, CEM III/B, CEM III/C, CEM IV, CEM V |  |  |  |  |  |  | 
CEM X
CEM X

## Slide 23: Content
Sustainability – Modern trends or duty of enterprise strategy?
Cement production and CO2 emission – CEM II and CEM III become standard
M-cements – optimised for performance, durability and uniformity
Rheology of cement paste vs. cement standard parameters
Rheology of cement paste – Experience from 5 years RheoZ
Summary

## Slide 24: Customer benefit analysis cement „Welche Nutzenfaktoren sind Ihnen am Zement/Lieferanten besonders wichtig?“
1. Quantitative assessment of benefit criteria:
1. Position Price (30%)
2. Position Product uniformity (13%)
.
. < 10% (Reliability, logistics, references, R & D, consulting, …)
.
„Very high evalution of product uniformity regarding customer benefits“
2. Improvement potentials for customer benefits:
„In all markets (ready-mix, conctruction elements, plaster and mortar) the improvement of product uniformity achieves the strongest positive effects amongst all criteria.“
(Except price reduction)

## Slide 25: Product strategy Dyckerhoff = . . . + Product uniformity
Product uniformity cement = Constant
Workability of cements (Cement paste)
Mechanical strength properties of the cements (hardened cement)
Durability of the cements (hardened cement)
Additional properties (Colour, fineness, composition,
rheological properties of dry cement,
heat development, etc.)

## Slide 26: Product uniformity
Increasing importance of product uniformity:
automated, fast production processes
increased quality requirements on final products concrete, …
Cost pressure at the cement customer (Minimisation of failures and reserves)
Increased rate of sensitive and softer concretes
Reduction of cement content in concrete
Increased application of concrete chemistry

## Slide 27: Produktgleichmäßigkeit Verarbeitungseigenschaften Beton
Workability of concrete:
Rheological properties of fresh concrete between mixing and setting (stiffening, concrete binding, …)
Rheological properties of fresh concrete are strongly dependent on the rheological properties of the fluid phase of the fresh concrete (mortar/cement paste)
Other influences: Concrete composition, mortar content, paste content
additives
temperature
.
.
Rheology/workability cement paste

## Slide 28
Workability parameters cement acc. DIN EN 196 Teil 3 Water demand, begin of setting
not relevant to practice
w/c 0,25 – 0,35 (without SP, „tamped
concrete“)
- static, insensitive method
- no continuous rheological
information during setting
Standard parameters are not the practical
workability parameters
In the market: Introduction of own methods
General critisism in the market regarding
workabilty

## Slide 29: Product uniformity – Workability of cement paste
Product uniformity
=
Uniformity of cement standard parameters
+
Uniformity of additional properties
Duty
+
Volantary

## Slide 30: Hydraulic binder rheology with the Viskomat NT
Principal:
Der Viskomat is a universal viscometer for measuring the consistancy/stiffness of fluid binder mixes.
The cement paste rotates in a pot mit with a fixed paddle. The torsional force is measured, depending on the stiffness of the cement paste.

## Slide 31: Rheometry cement paste with Viskomat NT
Ansteifen
Rücksteifen
Ansteifen
Rücksteifen

## Slide 32: Rheomety in quality control: Torque M = f (time t)

## Slide 33: Rheometry in quality control: Ansteifen/Rücksteifen = f (shipping date)
Ansteifen
Rücksteifen

## Slide 34: Changing workability
Kubens, Katz, Bentur, Wallevik, 2010

## Slide 35: Yield stress vs. heat development/reactivity clinker
Kubens, Wallevik, 2010

## Slide 36: Rheology laboratory Dyckerhoff
Approx. 3500 measurements per year:
-Quality control of all cement types
-Effect of additives
-Answering to customer complaints
-R & D
Cements with optimised workability and high uniformity

## Slide 37: Content
Sustainability – Modern trends or duty of enterprise strategy?
Cement production and CO2 emission – CEM II and CEM III become standard
M-cements – optimised for performance, durable and uniform
Rheology of cement paste vs. cement standard parameters
Rheology of cement paste – Experience from 5 years RheoZ
Summary

## Slide 38: RheoZ – Precision and accuracy Paste made with CEM I 52,5R (four cement mixes, four viscometers)
Chart: Paste with CEM I 52,5R Comparison of 4 viscometers

## Slide 39: RheoZ – Reference cement
Chart: Consistency/paste Reference cement

## Slide 40: RheoZ – Sensitivity temperature

## Slide 41: RheoZ – Sensitivity w/c-ratio

## Slide 42: RheoZ – Sensitivity technology (fineness)

## Slide 43: RheoZ – Sensitivity technology (fineness)
Chart: Rheological parameters/fineness
| 40451 | 40458 | 40465 | 40472 | 40479 | 40486 | 40493 | 40500 | 40507 | 40514 | 40521 | 40528 | 40542 | 40549 | 40554 | 40563 | 40570 | 40577 | 40584 | 40591 | 40598 | 40605 | 40612 | 40619 | 40626 | 40633 | 40640 | 40647 | 40654 | 40661 | 40668 | 40675 | 40682 | 40689 | 40695 | 40703 | 40710 | 40716 | 40724 | 40731 | 40738
Max-Min | 4.1124 | 6.3293 | 5.7639 | 5.8637 | 4.5557 | 4.9769 | 4.4892 | 5.376 | 5.3871 | 6.2295 | 4.8439 | 6.6396 | 5.5977 | 5.2762 | 4.6777 | 5.3982 | 4.1124 | 4.7996 | 4.6222 | 6.8613 | 5.2762 | 3.8352 | 4.9326 | 4.589 | 10.1065 | 9.8975 | 9.7545 | 10.0405 | 9.2377 | 12.4379 | 7.1262 | 9.6886 | 10.8653 | 7.5001 | 9.8095 | 9.9965 | 6.7743 | 10.3154 | 8.1599 | 8.9847 | 10.2494
M10 | 39.6992 | 41.4173 | 39.3057 | 35.6977 | 38.4577 | 38.1972 | 40.8242 | 41.445 | 34.9993 | 37.4102 | 36.0468 | 37.2772 | 37.7317 | 34.7887 | 36.5512 | 36.2297 | 34.3121 | 39.5939 | 38.3025 | 38.3413 | 40.8963 | 39.5163 | 41.5337 | 38.2803 | 67.8617 | 70.1601 | 73.8222 | 72.651 | 69.0769 | 73.8772 | 58.833 | 68.3291 | 70.2811 | 67.4548 | 58.701 | 66.9709 | 60.532 | 61.8957 | 68.3896 | 58.3491 | 66.7675 | 77.5668 | 68.6315 | 69.21 | 66.95 | 65.77 | 59.92 | 60.14 | 63.23 | 64.63 | 67.18 | 69.19 | 71.98
Blaine [cm°2/g] | 4760 | 4900 | 4820 | 4640 | 4650 | 4870 | 4930 | 4960 | 4820 | 4950 | 4860 | 4820 | 4750 | 4740 | 4830 | 4920 | 4920 | 4980 | 4980 | 5140 | 5200 | 5120 | 5190 | 6270 | 5980 | 6080 | 6180 | 6130 | 6060 | 5860 | 5770 | 5940 | 5700 | 5770 | 5930 | 5860 | 5920 | 5920 | 6040

## Slide 44: RheoZ – Sensitivity technology (common/separate milling CEM III/B 42,5 N)
Chart: Konsistenz/Leim (w/z=0,48)

## Slide 45: RheoZ - CEM III/B over a period of 2 years
Chart: Rheological parameters CEM III/B 42,5N-LH/HS/NA

## Slide 46: RheoZ – Sensitivity technology (gypsum phases)

## Slide 47: RheoZ – Sensitivity technology
Chart: Rheological parameters CEM I 52,5R, w/c=0,51
Start-up cement cooler

## Slide 48: Comparison CEM I 52,5 R – w/c rate constant 0,485

## Slide 49: Comparison CEM I 52,5 R – Consistence at beginning constant

## Slide 50: Content
Sustainability – Modern trends or duty of enterprise strategy?
Cement production and CO2 emission – CEM II and CEM III become standard
M-cements – optimised for performance, durable and uniform
Rheology of cement paste vs. cement standard parameters
Rheology of cement paste – Experience from 5 years RheoZ
Summary

## Slide 51: Summary
Sustainability = no modern trend, but duty of the enterprise strategy
CEM II and CEM III are the standard cements, CEM X will emerge
Dyckerhoff uses for composite cements S, LL, V and P
Seperate milling enables high performance, durability and uniformity of multi-component cements
M-cements combine the positive properties of clinker and composites
Part of the product strategy is the high uniformity (assessed with new measurement techniques for the optimisation of workability)
Five years Dyckerhoff RheoZ => Cements with high optimised uniformity regarding workability
Aim: To bridge the gap between cement rheology and rheology of mortar and concrete

## Slide 52: Thank you for your attention!
Heraklit - panta rhei – everything flows, even the mountains, you have to wait long enough